## Slide 2: The motivation
Artificial Hip implants only last about 10 years due to a process called aseptic loosening.
Wear debris causes both local and system-wide biological reactions
This research applies a novel titanium carbide (TIC) surface to a Ti64 substrate to reduce wear.
Specifically, this research examines the interface between the novel surface and the substrate to determine if it has desirable integration properties (i.e. a smooth transition)

## Slide 3: The Summary
First a thin film of TiC is applied to the Ti64 substrate using Microwave Plasma Assisted Chemical Vapor Deposition (MPACVD)
Then this research examines the surface using X-Ray Diffraction (XRD) and (AFM) to confirm that the carbide surface has been created and examine interface properties
Custom code is written to post process sample imagery
Computational methods (molecular dynamics) were used to model the movement of atoms in the interface
Finally, a mixture of molecular dynamics and Design of Experiments were used to model the application process

## Slide 4: Experimental Work

## Slide 5: Computational Work